Supporting Information

Molecular crowding agent engineering of bio-inspired electrolytes toward high-voltage aqueous supercapacitors

Mengke Peng1, Li Wang1, Longbin Li1, Zhongyou Peng1, Xiannong Tang1, Ting Hu1, Kai Yuan1*, Yiwang Chen1,2*

1College of Chemistry/Institute of Polymers and Energy Chemistry, Nanchang University, 999 Xuefu Avenue, Nanchang, 330031, China

2Institute of Advanced Scientific Research (iASR), Key Laboratory of Functional Small Molecules for Ministry of Education, Jiangxi Normal University, 99 Ziyang Avenue, Nanchang, 330022, China

E-mail address: kai.yuan@ncu.edu.cn, ywchen@ncu.edu.cn

Figures

Fig. S1. Optical image of molecular crowding electrolyte.

Fig. S2. Schematic diagram of ion transport of SCs using different electrolytes in discharged state. (a) the SC using 2 m LiTFSI electrolyte, (b) the SC using molecular crowding electrolyte.

Fig. S3. Photograph recording the burning of 2 m LiTFSI-100%PEG.

Fig. S4. (a) Nitrogen adsorption/desorption isotherms and (b) pore size distribution of the activated carbon.

The nitrogen adsorption-desorption isotherms were obtained using a Quantachrome Autosorbp-IQ at 77 K. The specific surface area was calculated using the Brunauer-Emmett-Teller (BET) theory. The pore size distribution was analyzed based on a combination of density functional theory (DFT).

Fig. S5. Electrochemical performance of the SC using 2 m LiTFSI-94%EG62 electrolyte. (a) Nyquist plots, (b) CV curves at a scan rate of 50 mV s-1 over an operation voltage range from 2.0 to 2.5 V, and (c) GCD curves at a current density of 0.2 A g-1 over an operation voltage range from 2.0 to 2.5 V.

Fig. S6. GCD curves at a current density of 0.2 A g-1 over an operation voltage range from 2.0 to 2.7 V of the supercapacitors using (a) 2 m LiTFSI-94%PEG400 and (b) 2 m LiTFSI-94%PEG600 electrolyte (CE: Coulombic efficiency).

Fig. S7. Equivalent circuit diagram of the symmetric SCs.

Rs corresponds to the solution resistance. Rct and Zw are the charge transfer resistance and the Warburg impedance, respectively. CPE1 denote the constant phase element. In Nyquist plots, the ﬁrst intersection with the x-axis at the highest frequency is mainly attributed to Rs. At higher frequencies, the diameter of the semicircle is attributed to Rct. At low frequencies, the sloping line represents the Warburg impedance.

In Fig. 2b, compared with the SCs using 2 m LiTFSI-94%PEG400 and 2 m LiTFSI-94%PEG600 electrolytes, the SC using 2 m LiTFSI-94%PEG200 electrolyte shows a much smaller equivalent series resistance. At low-frequency region, the 2 m LiTFSI-94%PEG200 electrolyte exhibits a nearly vertical line, indicating a fast ion diffusion in the active material and good capacitive behavior. At high-frequency region, the smaller semicircle and lower solution resistance (20.1 Ω) of the 2 m LiTFSI-94%PEG200 electrolyte, indicating the admirable charge transfer kinetics within the electrode and high ion transport in the solution, respectively. In comparison, the others exhibit limited transport process for electron and ion.

Fig. S8. Electrochemical performance of SCs using three different molecular crowding electrolytes. (a) CV curves at a scan rate of 50 mV s-1 over an operation voltage range from 2.0 to 2.7 V, (b) CV curves at different scan rates, and (c) GCD curves at different current densities of the SC using 2 m LiTFSI-94%PEG200 electrolyte. (d) CV curves at a scan rate of 50 mV s-1 over an operation voltage range from 2.0 to 2.7 V. (e) CV curves at different scan rates, and (f) GCD curves at different current densities of the SC using 2 m LiTFSI-94%PEG400 electrolyte. (g) CV curves at a scan rate of 50 mV s-1 over an operation voltage range from 2.0 to 2.7 V, (h) CV curves at different scan rates, and (i) GCD curves at different current densities of the SC using 2 m LiTFSI-94%PEG600 electrolyte.

Fig. S9. Schematic diagram of ion transport during charging in different electrolytes.

High ionic conductivity means fast ion transport, demonstrating small ion transport barriers. In the charging process, for example, 2 m LiTFSI-94%PEG200 has a high ionic conductivity, and the anions and cations are transferred to the surface and interior of the electrode at a rocket-like speed. By contrast, the ionic conductivity of 2 m LiTFSI-94%PEG400 and 2 m LiTFSI-94%PEG600 gradually decreases, and the corresponding ion transmission slows down, which is symbolized by the speed of car-like and motorcycle-like, respectively. Fast ion transport is conducive to fast ion storage and further helps to improve the charging speed and rate performance of SCs.

Fig. S10. Specific capacitance at different current densities of SCs using three different molecular crowding electrolytes under different temperatures. (a) 0 °C, and (b) 50 °C.

The applicable temperature range becomes a critical parameter for the energy storage device in practical applications and mainly depends on the electrolyte. Combined with the DSC measurement results, electrochemical performance of the SCs using 2 m LiTFSI-94%PEG200, 2 m LiTFSI-94%PEG400 and 2 m LiTFSI-94%PEG600 electrolytes at different temperatures were evaluated (Fig. S10, Supporting Information). At low temperature (0 °C), the SC using 2 m LiTFSI-94%PEG200 electrolyte can be applied at a larger current density of 1A g-1, which benefits from the lower glass-liquid transition temperature of the electrolyte. Under high temperature (50 °C), the SC using 2 m LiTFSI-94%PEG200 electrolyte possesses superior rate performance and retains 64% of its initial capacitance at 4 A g-1 (17.3 F g-1), higher than those of the SC using 2 m LiTFSI-94%PEG400 electrolyte (63%, 16.5 F g-1) and 2 m LiTFSI-94%PEG600 electrolyte (55%, 14.4 F g-1). Remarkably, speciﬁc capacitance of the SCs increases with increasing operation temperature owing to the enhancement of ionic kinetics. Therefore, the SC using 2 m LiTFSI-94%PEG200 electrolyte could be applied to a wide temperature range.

Fig. S11. Electrochemical performance of SCs using LiTFSI-based electrolytes. (a) CV curves at different scan rates, and (b) GCD curves at different current densities of the SC using 2 m LiTFSI electrolyte. (c) CV curves at different scan rates, and (d) GCD curves at different current densities of the SC using 21 m LiTFSI electrolyte. (e) Specific capacitance at different current densities of SCs using 2 m LiTFSI, 21 m LiTFSI and 2 m LiTFSI-94%PEG200 electrolytes. (f) Energy density at different current densities of SCs using LiTFSI-based electrolytes.

Fig. S12. Ragone plots of symmetric activated carbon-based supercapacitors.

Fig. S13. (a) Cycling stability of the SC using 2 m LiTFSI-94%PEG200 electrolyte at a current density of 1 A g-1, and (b) GCD curves of the last 10 cycles.

Fig. S14. Electrochemical performance of SCs using NaClO4-based electrolytes. (a) CV curves at different scan rates, and (d) GCD curves at different current densities of the SC using 1 m NaClO4 electrolyte. (b) CV curves at different scan rates, and (e) GCD curves at different current densities of the SC using 17 m NaClO4 electrolyte. (c) CV curves at different scan rates, and (f) GCD curves at different current densities of the SC using 1 m NaClO4-94%PEG200 electrolyte. (g) Nyquist plots, and (h) specific capacitance at different current densities of the SCs using NaClO4-based electrolytes. (i) Contact angle for 1 m NaClO4-94%PEG200 electrolyte on AC electrodes substrate. (j) Photograph recording the burning of 1 m NaClO4-94%PEG200 electrolyte.

Fig. S15. Electrochemical performance of SCs using LiClO4-based electrolytes. (a) CV curves at different scan rates, and (d) GCD curves at different current densities of the SC using 0.35 m LiClO4 electrolyte. (b) CV curves at different scan rates, and (e) GCD curves at different current densities of the SC using 5 m LiClO4 electrolyte. (c) CV curves at different scan rates, and (f) GCD curves at different current densities of the SC using 0.35 m LiClO4-94%PEG200 electrolyte. (g) Nyquist plots, and (h) specific capacitance at different current densities of the SCs using LiClO4-based electrolytes. (i) Contact angle for 0.35 m LiClO4-94%PEG200 electrolyte on AC electrodes substrate. (j) Photograph recording the burning of 0.35 m LiClO4-94%PEG200 electrolyte.

Fig. S16. Electrochemical performance of SCs using NaOTF-based electrolytes. (a) CV curves at different scan rates, and (d) GCD curves at different current densities of the SC using 1 m NaOTF electrolyte. (b) CV curves at different scan rates, and (e) GCD curves at different current densities of the SC using 7 m NaOTF electrolyte. (c) CV curves at different scan rates, and (f) GCD curves at different current densities of the SC using 1 m NaOTF-94%PEG200 electrolyte. (g) Nyquist plots, and (h) specific capacitance at different current densities of SCs using NaOTF-based electrolytes. (i) Contact angle for 1 m NaOTF-94%PEG200 electrolyte on AC electrodes substrate. (j) Photograph recording the burning of 1 m NaOTF-94%PEG200 electrolyte.

Fig. S17. Self-discharge curves of SCs using different electrolytes. Self-discharge curves of SCs using NaClO4-based electrolytes. (a) Self-discharge curves at individual maximum charging voltages, (b) potential retention curves at individual maximum charging voltages, (c) self-discharge curves at 1.6 V charging voltage. Self-discharge curves of SCs using LiClO4-based electrolytes. (d) Self-discharge curves at individual maximum charging voltages, (e) potential retention curves at individual maximum charging voltages, (f) self-discharge curves at 1.8 V charging voltage. Self-discharge curves of SCs using NaOTF-based electrolytes. (g) Self-discharge curves at individual maximum charging voltages, (h) potential retention curves at individual maximum charging voltages, (i) self-discharge curves at 1.8 V charging voltage.

Fig. S18. Cycling stability of SCs using three different molecular crowding electrolytes. (a) Cycling performance at a current density of 1 A g-1, and (b) GCD curves of the last 10 cycles of the SC using 1 m NaClO4-94%PEG200 electrolyte. (c) Cycling performance at a current density of 1 A g-1, and (d) GCD curves of the last 10 cycles of the SC using 0.35 m LiClO4-94%PEG200 electrolyte. (e) Cycling performance at a current density of 1 A g-1, and (f) GCD curves of the last 10 cycles of the SC using 1 m NaOTF-94%PEG200 electrolyte.

Fig. S19. Comparison of the electrochemical performance of SCs using different electrolytes at different temperatures. Comparison of (a) Nyquist plots, (b) CV curves at a scan rate of 50 mV s-1, and (c) GCD curves at a current density of 0.2 A g-1 of SCs using LiTFSI-based electrolytes at different temperatures. Comparison of (d) Nyquist plots, (e) CV curves at a scan rate of 50 mV s-1, and (f) GCD curves at a current density of 0.2 A g-1 of SCs using NaClO4-based electrolytes at different temperatures. Comparison of (g) Nyquist plots, (h) CV curves at a scan rate of 50 mV s-1, and (i) GCD curves at a current density of 0.2 A g-1 of SCs using LiClO4-based electrolytes at different temperatures. Comparison of (j) Nyquist plots, (k) CV curves at a scan rate of 50 mV s-1, and (l) GCD curves at a current density of 0.2 A g-1 of SCs using NaOTF-based electrolytes at different temperatures.

According to the results in Fig. S19 in the Supporting Information, compared with room temperature condition, the equivalent series resistance of these SCs is relatively reduced, which is due to the rapid ionic kinetics at high temperature. The CV curves of SCs using molecular crowding electrolytes show smaller polarization at 50 °C compared with the corresponding CV curves at 25 °C. This attributed to the fact that there is only a small amount of free water in the molecular crowding electrolytes, and the activity of water is relatively low under high temperature condition, which leads to almost little decomposition of water. On the contrary, the diluted solutions and high concentration electrolytes, especially the low concentration ones, are obviously polarized with increasing temperature. From the GCD curves of SCs using diluted solutions and high concentration electrolytes, it can be found that the original regular triangle had been deformed, even the original voltage window cannot reached, verifying the occurrence of the oxygen evolution reaction.[20] In contrast, the GCD curves of SCs using molecular crowding electrolytes deliver more symmetrical shape and exhibit a higher specific capacitance due to low water activity and rapid ionic kinetics. As a result, the superior high-temperature electrochemical performance of SCs using molecular crowding electrolytes demonstrate the feasibility to meet the demand for large-scale application under harsh environments.

Fig. S20. (a) Rate capability of 2.5 V SC pouch cell using 2 m LiTFSI-94%PEG200 electrolyte. (b) Photograph of the SC pouch cell.

SC pouch cell was assembled with AC mass loading of 72 mg on 90 cm2 stainless steel foil current collector and nonwoven fabric as separator. In Fig. 5b and Fig. S20 in the Supporting Information, this SC pouch cell delivers high speciﬁc capacitance values of 18.4, 15.5, 13.4 and 10.4 F g-1 at the current densities of 0.2, 0.5, 1 and 2 A g-1, respectively. The corresponding capacities are 2.6, 2.2, 1.9 and 1.5 F, energy densities are 16.3, 13.4, 11.6 and 9 Wh kg-1 at power densities of 270, 709, 1644 and 4563 W kg-1, respectively.

Tables

Table S1. Comparison of ionic conductivity, price of electrolytes and operation voltage of assembled devices.

| Electrolyte | Ionic conductivity (mS cm-1) | Operation voltage (V) | Aladdin (USD/10 mL) | Devices | Ref. |
| --- | --- | --- | --- | --- | --- |
| 2 m LiTFSI-94%PEG200 | 0.71 (25 ℃) | 0-2.5 | 3.687 | AC//AC | This Work |
| 2 m LiTFSI-94%PEG400 | 0.35 (25 ℃) | 0-2.5 | 3.687 | AC//AC | This Work |
| 2 m LiTFSI-94%PEG600 | 0.28 (25 ℃) | 0-2.5 | 3.687 | AC//AC | This Work |
| 1 m NaClO4-94%PEG200 | 0.90 (25 ℃) | 0-2.5 | 0.244 | AC//AC | This Work |
| 0.35 m LiClO4-94%PEG200 | 0.57 (25 ℃) | 0-2.5 | 0.212 | AC//AC | This Work |
| 1 m NaOTF-94%PEG200 | 0.60 (25 ℃) | 0-2.5 | 2.395 | AC//AC | This Work |
| 21 m LiTFSI | 8.1 (25 ℃) | 0-2.1 | 37.5 | AC//AC | This Work |
| 17 m NaClO4 | >20 (25 ℃) | 0-2.1 | 2.165 | AC//AC | This Work |
| 5 m LiClO4 | >20 (25 ℃) | 0-2.0 | 1.362 | AC//AC | This Work |
| 7 m NaOTF | >20 (25 ℃) | 0-2.0 | 15.95 | AC/AC | This Work |
| 21 m LiTFSI-7 m LiOTF | 6.5 (25 ℃) | 0.8-2.5 | 45 | LiMn2O4//c-TiO2 | [1] |
| 19.4 m LiTFSI-8.3 m LiBETI | 3.0 (30 ℃) | 1.8-2.4 2.8-3.1 | 2805 | LiCoO2//Li4Ti5O12 LiNi0.5Mn1.5O4//Li4Ti5O12 | [2] |
| 22.2 m LiTFSI-33.3 m LiPTFSI | 0.1 (30 ℃) | 1.8-2.8 | N | LiCoO2/Li4Ti5O12 | [3] |
| 32 m KOAc-8 m LiOAc | 5.3 (25 ℃) | 0.7-2.5 | 0.87 | LiMn2O4//c-TiO2 | [4] |
| 42 m LiTFSI + 21 m Me3EtN·TFSI | 0.86 (25 ℃) | 1.8-2.8 | N | LiMn2O4//Li4Ti5O12 | [5] |
| NaClO4/(H2O)1.5(ACN)2.4 | 41.2 (25 ℃) | 0-2.5 | 1.645 | AC//AC | [6] |
| LiTFSI/H2O/(ACN)3.5 | 13.2 (25 ℃) | 0-2.4 | 13.572 | AC//AC | [7] |
| LiFSI/(H2O)0.69(EC)0.35(DMC)0.28 | 3.78 (25 ℃) | 0-2.5 | 156.2 | AC//AC | [8] |
| NaOTF/(H2O)/(PC) | 25 (20 ℃) | 0.5-1.5 | 17.832 | Na3V2(PO4)3//NaTi2(PO4)3 | [9] |

Table S2. Comparison of price of commonly used chemicals in electrolytes.

| Chemical | Aladdin (USD/g) | TCI (USD/g) |
| --- | --- | --- |
| PEG200 | 0.013 | 0.086 |
| PEG400 | 0.013 | 0.1 |
| PEG600 | 0.013 | 0.086 |
| LiTFSI | 0.622 | 2.93 |
| NaClO4 | 0.104 | N |
| LiClO4 | 0.256 | N |
| NaOTF | 1.324 | 6.196 |
| LiOTF | 0.691 | 3.515 |
| LiBETI | 86.24 | 75.96 |
| LiPTFSI | N | N |
| KOAc | 0.013 | 0.224 |
| LiOAc | 0.088 | 0.177 |
| Me3EtN·TFSI | N | N |
| LiFSI | 5.49 | 118 |
| ACN | 0.29 | 0.06 |
| EC | 0.02 | 0.08 |
| DMC | 0.02 | 0.08 |
| PC | 0.15 | 0.08 |

References

[1]	L. Suo, O. Borodin, W. Sun, X. Fan, C. Yang, F. Wang, T. Gao, Z. Ma, M. Schroeder, A. Cresce, S. M. Russell, M. Armand, A. Angell, K. Xu, C. Wang, Angew. Chem., Int. Ed. 2016, 55, 7136.

[2]	Y. Yamada, K. Usui, K. Sodeyama, S. Ko, Y. Tateyama, A. Yamada, Nat. Energy 2016, 1, 16129.

[3]	S. Ko, Y. Yamada, K. Miyazaki, T. Shimada, E. Watanabe, Y. Tateyama, T. Kamiya, T. Honda, J. Akikusa, A. Yamada, Electrochem. Commun. 2019, 104, 106488.

[4]	M. R. Lukatskaya, J. I. Feldblyum, D. G. Mackanic, F. Lissel, D. L. Michels, Y. Cui, Z. Bao, Energy Environ. Sci. 2018, 11, 2876.

[5]	L. Chen, J. Zhang, Q. Li, J. Vatamanu, X. Ji, T. P. Pollard, C. Cui, S. Hou, J. Chen, C. Yang, L. Ma, M. Ding, M. Garaga, S. Greenbaum, H. S. Lee, O. Borodin, K. Xu, C. Wang, ACS Energy Lett. 2020, 5, 968.

[6]	Q. Dou, Y. Lu, L. Su, X. Zhang, S. Lei, X. Bu, L. Liu, D. Xiao, J. Chen, S. Shi, X. Yan, Energy Storage Mater. 2019, 23, 603.

[7]	D. Xiao, Q. Dou, L. Zhang, Y. Ma, S. Shi, S. Lei, H. Yu, X. Yan, Adv. Funct. Mater. 2019, 29, 1904136.

[8]	W. Wang, W. Deng, X. Wang, Y. Li, Z. Zhou, Z. Hu, M. Xue, R. Li, Chem. Commun. 2020, 56, 7965.

[9]	H. Zhang, B. Qin, J. Han, S. Passerini, ACS Energy Lett. 2018, 3, 1769.